## Slide 1
Introduction to Neutron Diffraction
Juan Rodríguez-Carvajal
Diffraction Group at ILL
Institut Laue Langevin, 71 avenue des Martyrs, CS 20156, 38042 Grenoble (France)

## Slide 2
Outline
Characteristics of neutrons for diffraction
Diffraction equations: Laue conditions
Comparison neutrons – synchrotron X-rays
Magnetic neutron diffraction
Examples of neutron diffraction studies

## Slide 3
Neutrons for what?
Neutrons tell you “where the atoms are and what the atoms do” (Nobel Prize citation for Brockhouse and Shull 1994)

## Slide 4
Particle-wave properties energy-velocity-wavelength ...
kinetic energy (E) velocity (v) temperature (T).
k= 2p/l = mnv/ħ
E= mnv2/2= kB T = p2/2mn= (ħk)2/2mn=(h/l)2/2mn
wavevector (k)
wavelength (l)
momentum (p)
ħ=h/2p
p= mnv = ħ k

## Slide 5
Neutrons, a powerful probe
Matter is made up atoms, aggregated together in organised structures
The properties of matter and materials are largely determined by their structure and dynamics (behaviour) on the atomic scale
distance between atoms ~ 1 Å = 1/100 000 000 cm Atoms are too small to be seen with ordinary light
(wavelength approx. 4000-8000 Å)
The wavelength of the neutron is comparable to atomic sizes and the dimensions of atomic structures, which explains why neutrons can « see » atoms.
The energy of thermal neutrons is similar to the thermal excitations in solids.
Neutrons are zero-charge particles and have a magnetic moment that interacts with the magnetic dipoles in matter.
Techniques using neutrons can produce a picture of atomic and magnetic structures and their motion.

## Slide 6
E = mnv2/2 = kB T = (ħk)2/2mn ; k = 2p/l = mnv/ħ
Energy (meV) Temp (K) Wavelength (Å)
Cold 0.1 – 10 1 – 120 4 – 30
Thermal 5 – 100 60 – 1000 1 – 4
Hot 100 – 500 1000 – 6000 0.4 – 1
Particle-wave properties (Energy-Temperature-Wavelength)
Cold Sources
COLD
THERMAL
HOT

## Slide 7
Scattering power of nuclei for neutrons
Light atoms diffuse neutrons as strongly as heavy atoms
The scattering power for X-rays is proportional to the atomic number (number of electrons).
The scattering power for electrons depends on the electrostatic potential
The scattering power for neutrons is of the same order of magnitude similar for all atoms

## Slide 8
Neutrons are strongly scattered by magnetic materials
Ferromagnetic and
antiferromagnetic oxides
Neutrons act as small magnets
The dipolar magnetic moment of the neutron interacts strongly with the atomic magnetic moment
Neutrons allow the determination of magnetic structures of materials and measure the magnetization with high precision.
Neutrons for magnetism studies
Magnetic Crystallography

## Slide 9
Outline
Characteristics of neutrons for diffraction
Diffraction equations: Laue conditions
Comparison neutrons – synchrotron X-rays
Magnetic neutron diffraction
Examples of neutron diffraction studies

## Slide 10
Interaction neutron-nucleus
= number of incident neutrons /cm2 / second
= total number of neutrons scattered/second/
Fermi’s golden rule gives the neutron-scattering Cross-section
 number of neutrons of a given energy scattered per second in a given solid angle
(the effective area presented by a nucleus to an incident neutron)
k
Direction
q, f
q
r
dS
z
k’
Target
dW
f

## Slide 11
Interaction neutron-nucleus
Fermi Pseudo potential of a nucleus in rj
The range of nuclear force (~ 1fm) is much less than neutron wavelength so that scattering is “point-like”
Weak interaction with matter aids interpretation of scattering data
Potential with
a single parameter
Plane wave
e ik·x
Sample
V(r)
k
Plane wave
e ik’·r
k’
r
Detector
k
Q
Spherical wave
(b/r)e ik·r
k’
2q

## Slide 12: Diffraction Equations
For diffraction part of the scattering the Fermi’s golden rule resumes to the statement: the diffracted intensity is the square of the Fourier transform of the interaction potential
There are different conventions and notations for designing the scattering vector (we use here crystallographic conventions).
Atomic form factor.
Scattering length

## Slide 13: Diffraction Equations for crystals
In a crystal the atoms positions can be decomposed as the vector position of the origin of a unit cell plus the vector position with respect to the unit cell
Laue conditions: the scattering vector is a reciprocal lattice vector of the crystal
integer

## Slide 14: Diffraction Equations for crystals
The Laue conditions have as a consequence the Bragg Law
Laue conditions: the scattering vector is a reciprocal lattice vector of the crystal

2

## Slide 15
From Pecharsky and Zavalij
Detector
Ewald construction
s0L/
sL/

## Slide 16
zL
yL
xL
Incident beam
1/
sL
s0L
2
h
crystal
xD
zD
OD


P
D
D
O
Ewald Sphere
Ewald construction
Laboratory Frame and detector

## Slide 17
Diffraction patterns
Single Xtal - 2D image + scan –> 3D Int vs 2θ
Powder - 2D image –> 1D Int vs 2θ
Courtesy of Jim Britten
nλ=2d(sinθ)
Single Crystal
Powder or polycrystalline solid

## Slide 18
From Pecharsky and Zavalij
Detector
Ewald construction Laue
s0L/
sL/
1/max
1/min

## Slide 19: Laue image obtained in Cyclops

## Slide 20: Single Crystal and Powder Diffraction
Single Crystal diffraction allows to get with high precision subtle structural details: thermal parameters, anharmonic vibrations.
Drawbacks: big crystals for neutrons, extinction, twinning
Data reduction: Needs only the indexing and integration of Bragg reflection and obtain structure factors. List: h k l F2 σ(F2)
Data Treatment: SHELX, FullProf, JANA, GSAS, …
Powder diffraction no problem with extinction or twinning.
Data reduction: minimalistic, needs only the profile intensities and their standard deviations
Data Treatment: FullProf, JANA, GSAS, TOPAS, …

## Slide 21
Outline
Characteristics of neutrons for diffraction
Diffraction equations: Laue conditions
Comparison neutrons – synchrotron X-rays
Magnetic neutron diffraction
Examples of neutron diffraction studies

## Slide 22: Why neutrons?
NEUTRON DIFFRACTION FOR FUNDAMENTAL AND APPLIED RESEARCH IN CONDENSED MATTER AND MATERIALS SCIENCE
Location of light elements and distinction between adjacent elements in the periodic table.
Examples are:
Oxygen positions in High-TC superconductors and manganites
Structural determination of fullerenes an their derivatives,
Hydrogen in metals and hydrides
Lithium in battery materials
Determination of atomic site distributions in solid solutions
Systematic studies of hydrogen bonding
Host-guest interactions in framework silicates
Role of water in crystals
Magnetic structures, magnetic phase diagrams and magnetisation densities
Relation between static structure and dynamics (clathrates, plastic crystals).
Aperiodic structures: incommensurate structures and quasicrystals

## Slide 23
The complementary use of X-ray Synchrotron radiation and neutrons (1)
The advantages of thermal neutrons with respect to X-rays as far as diffraction is concerned are based on the following properties of thermal neutrons:
  constant scattering power (b is Q-independent) having a non-monotonous dependence on the atomic number
  weak interaction (the first Born approximation holds) that implies simple theory can be used to interpret the experimental data
  the magnetic interaction is of the same order of magnitude as the nuclear interaction
  low absorption, making it possible to use complicated sample environments
Why neutrons?

## Slide 24: Why neutrons?
  Powder diffraction with SR can be used for ab initio structure determination and microstructural analysis due to the current extremely high Q-resolution.
  Structure refinement is better done with neutrons (or using simultaneously both techniques) because systematic errors in intensities (texture effects) are less important and because scattering lengths are Q-independent in the neutron case.
The complementary use of X-ray Synchrotron radiation and neutrons (2)

## Slide 27: Why neutrons?
  Magnetic X-ray scattering allows in principle the separation of orbital and spin components. However, SR cannot compete with neutrons in the field of magnetic structure determination from powders.
  The contribution of SR to that field is on details of magnetic structures (already known from neutrons) for selective elements using resonant magnetic scattering (rare earths, U, ...)
The complementary use of X-ray Synchrotron radiation and neutrons (3)

## Slide 28
Outline
Characteristics of neutrons for diffraction
Diffraction equations: Laue conditions
Comparison neutrons – synchrotron X-rays
Magnetic neutron diffraction
Examples of neutron diffraction studies

## Slide 29
Magnetic scattering: magnetic fields
The interaction potential to be evaluated in the FGR is:
Magnetic field due to spin and orbital moments of an electron:
O
Rj
sj
j
pj
R
R+Rj
Bj
Magnetic vector potential of a dipolar field due to electron spin moment
Biot-Savart law for a single electron with linear momentum p
Electron
Neutron

## Slide 30
Magnetic scattering: magnetic fields
Evaluating the spatial part of the transition matrix element for electron j:
Where is the momentum transfer
Summing for all unpaired electrons we obtain:
M(Q) is the perpendicular component of the Fourier transform of the magnetisation in the scattering object to the scattering vector. It includes the orbital and spin contributions.

## Slide 31
Scattering by a collection of magnetic atoms
We will consider in the following only elastic scattering.
We suppose the magnetic matter made of atoms with unpaired electrons that remain close to the nuclei.
Vector position of electron e:
The Fourier transform of the magnetization can be written in discrete form as

## Slide 32
If we use the common variable s=sin/, then the expression of the form factor is the following:
Scattering by a collection of magnetic atoms

## Slide 33
M(Q) is the perpendicular component of the Fourier transform of the magnetisation in the sample to the scattering vector.
Magnetic interaction vector
Magnetic structure factor:
Neutrons only see the components of the magnetisation that are perpendicular to the scattering vector
M
M 
Q=Q e
Magnetic scattering

## Slide 34
Elastic Magnetic Scattering by a crystal
For a general magnetic structure that can be described as a Fourier series:
The lattice sum is only different from zero when h-k is a reciprocal lattice vector H of the crystallographic lattice. The vector M is then proportional to the magnetic structure factor of the unit cell that now contains the Fourier coefficients Skj instead of the magnetic moments mj.

## Slide 35
Diffraction Patterns of magnetic structures
Magnetic reflections: indexed by a set of propagation vectors {k}
h is the scattering vector indexing a magnetic reflection
H is a reciprocal vector of the crystallographic structure
k is one of the propagation vectors of the magnetic structure
( k is reduced to the Brillouin zone)
Portion of reciprocal space
Magnetic reflections
Nuclear reflections
h = H+k

## Slide 36
Diffraction Patterns of magnetic structures
Cu2+ ordering
Ho3+ ordering
Notice the decrease of the paramagnetic background on Ho3+ ordering

## Slide 37: Magnetic refinement on D2B

## Slide 38
Outline
Characteristics of neutrons for diffraction
Diffraction equations: Laue conditions
Comparison neutrons – synchrotron X-rays
Magnetic neutron diffraction
Examples of neutron diffraction studies

## Slide 39
Two Axes Diffractometers: Powders and Liquids
High Resolution D2B
Low Resolution
D20

## Slide 40
Real time powder diffraction on D1B
MoO3·H2O
T = 60 ºC
MoO3
T = 150 ºC
MoO3·2H2O
RT
Dehydration of MoO3·2H2O [N. Boudjada et al.; J. Solid State Chem. 105, 211 (1993)]
RT to 400 ºC in vacuum.
Diffraction pattern / 3 minutes.

## Slide 41
Some Applications: Liquid state  D4
Earth
Mars
Io
Ganymede
What they have in common …?
Fluid Outer Core: from 3000 to 5200 km
Primarily Fe with some Ni
Metallic cores
Proximity in Solar System
Thanks to Gabriel Cuello

## Slide 42
Some Applications: Liquid state
But r is 5-10% less than pure Fe+Ni …
… there is some light element, but which? S? O? H? Si?
Fe Ni
M. Nasch, M. H. Manghnani, R. A. Secco, Science 277 (1997) 219.
Hypothesis:
The light element helps aggregating clusters, which in turn are disaggregated by heating the system.
Volcanic
Eruptions

## Slide 43
Some Applications: Liquid state
FeNi and FeNiS alloys
Liquid state
High temperature
Special furnace
Two-axis diffractometer
Fe85Ni15
Fe−Fe
Fe85Ni5S10
Fe−Fe

## Slide 44: Levitation of Liquids
Pyrometer
Video camera
Mirror
Sample
Levitator
Gas flow
CO2 Laser
Principle of the aerodynamic levitation and laser heating

## Slide 45: Crystallisation
Neutron beam
Laser
Laser
Gas
Cold Point
CO2 laser
Laser beam
2nd mirror
Pyrometer
Neutron beam
1st mirror
Sample

## Slide 46: Again Crystallisation
Neutron beam
Laser
Dust coming from the sample
B4C Screen
Gas
Crystallisation due to contacts
Solutions:
Improvement of the levitation
Use of a screen in front of the nozzle
Neutron beam
Laser beams
B4C screens
Gas

## Slide 47: High Temperature Setup
NaCl window
Spherical mirror
Laser
Video Camera
Video Camera
Pyrometer
B4C screens
Sample

## Slide 48: Three Lasers Setup
Neutron beam
Laser 1
B4C screens
Gas
Detector
Laser 2
Laser 3
NaCl window

## Slide 49: Self-propagating High-T Synthesis (SHS) D20
Titanium silicon carbide Ti3SiC2
Self-propagating High-temperature Synthesis (SHS)
  Riley, Kisi et al.: 3 Ti : 1 Si : 2 C, 20 g pellet in furnace
  Heating from 850 C to 1050 C at 100 K/min
  Acquisition time 500 ms (300 ms)
Hot isostatic pressing expensive
2theta
time/s
counts/s/0.1°
2.3e4
0.1e4
30
0
25°
35°
2theta
time/s
counts/s/0.1°
2.3e4
0.1e4
70
-130
25°
35°
D.P. Riley, E.H. Kisi, T.C. Hansen, A. Hewat, J. Am. Ceramic Soc. 85 (2002) 2417-2424.
Thanks to
Thomas Hansen
Notes: Titanium silicon carbide, Ti3SiC2, has attracted considerable interest because of a unique combination of physical properties: a high melting point, good high temperature strength, resistance to corrosion and oxidation, high Young’s Modulus, and high electrical/thermal conductivity, characteristics, which are both metallic and ceramic in nature.
Ti3SiC2 has a hexagonal crystal structure consisting of double layers of TiC octahedra separated by a planar Si layer. Band structure calculations indicate that ionic, covalent and metallic bonds co-exist within the structure. Potential applications include machinable structural ceramics that are corrosion, creep and oxidation resistant; corrosion and oxidation resistant barrier coatings; intermediate phases in metal-ceramic bonding; electrodes in electrochemical cells e.g. in aluminium smelting; and conducting films on dielectric and semi-conductor devices. The primary difficulty in realising these diverse applications is that, in common with all ternary or higher order phases, it has proven difficult to synthesise without unwanted ‘impurity’ phases. The properties of these impurity phases (e.g. TiCx and TixSiy type) are very different from those of Ti3SiC2, hence the properties of the final ceramic suffer.
The reactive sintering/hot isostatic pressing process is costly and difficult to scale up. In SHS the heat of reaction provides all of the thermal energy required, the reaction times are very short, and the industrial scale-up is straightforward. However, the products are usually very porous and of lower purity.
In order to optimise an SHS method it is important to focus on the mechanisms that control the growth of Ti3SiC2 as a product phase. Because of the great speed of the SHS reactions and the very high temperatures involved,the mechanisms are generally poorly understood because sample characterisation has been reliant on post-reaction techniques. Mechanisms for Ti3SiC2 formation by reactive sintering have been developed by these ex-situ methods. In-situ observations of SHS reactions have been successfully performed on several binary systems using synchrotron X-ray diffraction. This has provided valuable insight into the systems studied however there are still some unresolved problems. The synchrotron studies to date use ccd detectors with very limited angular range. In addition, the X-rays used are heavily absorbed by the sample, usually within some tens of microns of the surface. SHS reactions are widely known to cause volatilisation of some chemical species due to the high reaction temperatures attained. In the Ti-Si-C system, the major losses are thought to be Si. It is therefore unclear whether the surface of the sample would be truly representative of the bulk. In order to overcome these shortcomings, we have used neutron diffraction to study the SHS reaction of 3Ti/SiC/C mixtures and demonstrate an entirely new reaction mechanism.
Experimental
Stoichiometric 3Ti:1Si:2C powder mixtures of Ti powder (Sigma-Aldrich, -325mesh, 99.98%), SiC powder (Performance Ceramics Japan, <100m, 99.9%) and graphite powder (Aldrich, <100m, 99.9%) were mixed by hand in a mortar and pestle under an inert argon atmosphere (<5ppm 02, <10ppm H20). A schematic diagram of the sample environment is shown in Figure 1. Two or three  6g pellets 12.2mm high and 15.2mm in diameter were prepared by cold-pressing at 180 MPa in a steel die. The pellets were stacked and placed at the centre of a 16mm inner diameter (ID) silica (SiO2) tube with a wall thickness of 1.5mm. An insulating section of Al2O3 was place atop a stainless steel support stand with a 3mm thick Ti disc separating the sample from the ceramic. Primary heating, ignition and neutron diffraction data collection were all conducted in a resistive vanadium vacuum furnace operating under a pressure of ~10-2 mbar. The sample and silica tube, were placed at the centre of an interchangeable (V or Nb), 20mm ID heating element (20-40m thick). A boron carbide (B4C) mask positioned 3200mm from the main reactor aperture and 50mm from the sample focal plane limited the neutron beam height to 42mm with a divergence of 3mm. Care was taken to ensure the support stand, Ti disc, and Al2O3 section, were well outside the penumbra of the neutron beam. K-type thermocouples were positioned ~3mm below the base of the Ti disc and used to control the furnace temperature. These also gave a crude capacity to monitor the exothermic ignition of the sample. Neutron diffraction patterns were recorded on the D20 diffractometer at the Institut Max von Laue-Paul Langevin, Grenoble, France, using a neutron wavelength of 1.300790.00007Å. The instrument is equipped with a micro-strip position sensitive detector allowing simultaneous detection of a diffraction patterns in the range 10 – 140o 2 .
A high intensity diffraction pattern was recorded at room temperature from each starting mixture. Samples were then pre-heated from room temperature to 400oC at 30oC/min. Between 400oC and 850oC the heating rate was maintained at 30oC/min. During this temperature interval, neutron diffraction patterns were collected for 5s each with an average dead time of 1s for data transfer. From 850oC to 1050oC the heating rate was increased to 102oC/min and the data acquisition time was decreased to 0.9s including 0.4s data transfer time. SHS ignition and combustion reactions occurred towards the latter part of this interval. Data collection was terminated approximately 15-20 minutes after ignition of the self-propagating reaction. [Three samples were studied, 2 in SiO2 and 1 without!]
Post-reaction products were examined using optical microscopy, SEM and XRD (Cu K). Diffraction patterns were analysed using the Rietveld analysis program Fullprof [ref]. Refined parameters for major phases were typically a zero correction, scale factors, peak shape parameters, atomic occupancies and lattice parameters. An interpolated fixed background was used to account for the presence of amorphous scattering from the silica tubing. This profile was obtained from the room temperature reactants pattern with minor modifications for the influence of increasing temperature. Visual analysis of phase transformations and the reaction mechanism were obtained using the Large Array Manipulation Program(LAMP) [ref].
Results
3.1 Reaction Overview
  Due to the excellent time resolution of the experiment (0.5s to record each diffraction pattern and 0.4s for data download), there is an enormous amount of data to analyse. An excellent overview of the time evolution of the experiment is shown in composite diagrams such as Figure 2(a). In Figure 2(a), time is shown on the vertical axis and the diffraction angle (2) on the horizontal axis. Increased brightness indicates increased intensity within the diffraction pattern. Select diffraction patterns showing important stages of the reaction are shown in Figure 2(b). Corresponding positions for patterns A, B, C, D and E are indicated in Figure 2(a) by the horizontal marks. Diffraction peak positions in Figure 2(b) may be cross-referenced directly with Figure 2(a) as they have the same 2 scale. Five distinct stages may be observed to occur in the samples and these may be represented by the diffraction patterns in Figure 2(b). These respectively represent (A) the initial reactants, (B) the start of the -Ti  -Ti transformation, (C) a pre-ignition stage between the completion of the -Ti  -Ti transformation and the ignition event, (D) the rapid evolution of an intermediate phase, and (E) the formation of the product phase, Ti3SiC2. Rietveld analysis results for these five patterns are shown in Table 1 and will be discussed in turn below.
Table 3.* Rietveld Quantitative Phase Analysis Results (%)
- Table of Rietveld results
  3.2 Stage 1 - Initial reactants
The diffraction pattern of each sample at room temperature consists of the reactant powders, -Ti, SiC and graphite as represented by pattern A in Fig 2(b). The presence of an amorphous background (eg at 14-22o 2) is attributable to the silica tubing surrounding the sample. This was readily accounted for in the Rietveld analysis via a fixed-point background. Below ### C the neutron diffraction patterns show only the expected thermal expansion of the reactant phases. This allows an estimate of the sample temperature to be made based on the lattice expansion.
QPA agrees with the starting stoichiometry.

## Slide 50: SHS: pre-ignition
26
28
30
34
-100
-50
0
32
50
2 theta/degrees
Ti a-b transition
  starting at 870 C
Pre-ignition:
  TiCx growth during 1 min
Melting (?) in 0.5 s
Notes: The transformation of -Ti to the  polymorph is the first significant change in the samples. It is most easily observed by the decrease in the intensity of the diffraction peak at 32.2 degrees and the corresponding increase in the intensity of the peak at 31.2 degrees. Quantitative phase analysis using Rietveld refinement scale factors indicate the completion rate of the transformation precisely. Using the thermal expansion of the reactants to calculate the temperature of the sample, it was estimated that the -Ti  -Ti transformation began at 870 C. The complete -Ti  -Ti transformation occurs over a certain temperature interval, due to a temperature gradient from the surface to the centre of the sample. The transformation rate is hence controlled by the thermal conductivity of the pellet. Other than this obvious phase transformation, there are no significant changes in the phase composition of the samples prior to the completion of the -Ti  -Ti transformation).
Between the end of the -Ti  -Ti transformation and the SHS ignition, over a period of around one minute, there are small but significant changes to the diffraction patterns. There is an increase in the intensity of the peak near 30 degrees. This peak is the major reflection from SiC, however it overlaps with TiC. There is an associated decrease in the intensity of the -Ti reflections (eg at 31.2o). Analysis of the complete diffraction patterns in this region using Rietveld refinements confirms the growth of a TiCx phase at the expense of -Ti and free carbon.

## Slide 51: SHS: intermediate product
26
28
30
34
-100
-50
0
32
50
2 theta/degrees
Intermediate phase
  TiC, Si substituted
  formed in 0.5 s, 2s delay
  Heating up to 2500 K
  afterwards decay in 5 s
Notes: In less than 0.9s, the entire 20g samples convert converted to a single solid phase with a NaCl structure not unlike TiC. This was confirmed by Rietveld analysis. The intermediate phase is a Si substituted TiC with approximately the same stoichiometry as the overall sample.
The SHS ignition event is readily seen in Figures 2(a) and 3 as a complete discontinuity in the diffraction signal. A closer view of the ignition event is shown in Figure 4(or5?) for one of the samples. In less than 0.9s, the reactant diffraction patterns were replaced by patterns like pattern D in Fig 2(b). The entire 20g samples had apparently converted to a single solid phase with a NaCl structure not unlike TiC. This was confirmed by Rietveld analyses such as the one shown in Figure 5 (or 6?). The intermediate phase is believed to be a Si substituted TiC with approximately the same stoichiometry as the overall sample. Details of the structure and significance of the intermediate phase will be discussed in section 4.3.
The intermediate phase persisted as the only solid phase for six seconds after the ignition event before nucleation and growth of the product phase began. An estimate of the sample temperature during and following SHS ignition was made using the lattice contraction of the intermediate phase on cooling. The lattice parameter at the end of the experiment was used as a reference on the assumption that the sample had cooled to be at the same temperature as the furnace. The thermal expansion coefficient used is that for pure TiC [ref] and may be slightly in error due to Si substitution. The resulting temperature profile is shown in Figure 6(7?) illustrating a maximum of 2500K. The temperature had decreased to approximately ____K before the Ti3SiC2 product phase was observed in the diffraction patterns.
  In the sample without the SiO2 tube this time was reduced to four seconds.

## Slide 52: SHS: final product
26
28
30
34
-100
-50
0
32
50
2 theta/degrees
Product Ti3SiC2
  starts after 5 s incubation
  time constant about 5 s
Notes: After the six-second incubation time, the product phase Ti3SiC2 begins to appear in the diffraction patterns at the upper end of Figs 2(a) and 4(5?). The rate of growth is quite rapid and is more clearly illustrated in Figure 3. After only a further 16 seconds or so, 80% of the sample has converted to the product phase and there is little further growth of product phase thereafter. The sample temperature at this time is estimated to have been __-__K. The amount of intermediate phase remaining at the end of the reaction is similar to the amount of TiCx formed in the pre-ignition stage

## Slide 53: Diffraction patterns of LaMnO3 vs Pressure (ISIS, POLARIS + Paris-Edinburgh cell)
Stability of the Janh-Teller effect and magnetic study of LaMnO3 under pressure
L. Pinsard-Gaudart, J.Rodriguez-Carvajal, A. Daoud-Aladine, I.N.Goncharenko, M. Medarde, R.I. Smith and A. Revcolevschi. PRB 64, 064426 (2001)

## Slide 54: Diffraction patterns of LaMnO3 vs Pressure (ISIS, POLARIS + Paris-Edinburgh cell)
Stability of the Janh-Teller effect and magnetic study of LaMnO3 under pressure
L. Pinsard-Gaudart, J.Rodriguez-Carvajal, A. Daoud-Aladine, I.N.Goncharenko, M. Medarde, R.I. Smith and A. Revcolevschi. PRB 64, 064426 (2001)
Rietveld refinement of LaMnO3 at RT and 14.6 kbar
In this range of pressure the reflections in the diffraction pattern are still sharp enough for performing a proper refinement

## Slide 55: LaMnO3 vs Pressure (ISIS, POLARIS + Paris-Edinburgh cell)
Behaviour of different structural parameters of LaMnO3 up to 70kbar

## Slide 56: Magnetic scattering of LaMnO3 vs Pressure (LLB, G61 + Goncharenko cell)
Rietveld refinement of the nuclear (fixed) and magnetic scattering of LaMnO3
The analysis of the magnetic contribution to the diffraction patterns indicates that the mode A continues to be dominant for all pressure range studied. However the mode Ay is unable to explain the diffraction pattern at 67 kbar.
The magnetic structure corresponds to the mixture of two representations
Γ3g(+-) and Γ4g(--) of Pbnm for k=0
[Gx,Ay, Fz] ~ [0,Ay, 0] and [Cx,Fy,Az] ~ [0,0,Az]
Magnetic structure at 67 kbar: [0,Ay,Az]

## Slide 57: Magnetic scattering of LaMnO3 vs Pressure (LLB, G61 + Goncharenko cell)
Magnetic structure vs pressure

## Slide 58: Conclusions LaMnO3
1: The main effect of pressure is to decrease the orthorhombic distortion by diminishing the tilt angle MnO6 octahedra (the interatomic distances diminish near isotropically)
Stability of the Janh-Teller effect and magnetic study of LaMnO3 under pressure
L. Pinsard-Gaudart, J.Rodriguez-Carvajal, A. Daoud-Aladine, I.N.Goncharenko, M. Medarde, R.I. Smith and A. Revcolevschi. PRB 64, 064426 (2001)
2: The Jahn-Teller effect is stable up to 70 kbar
3: The magnetic structure conserve the A-type of ordering but with a deviation of the magnetic moment from the b-axis towards the c-axis

## Slide 59
Thank you for your attention
www.neutron.anl.gov